## Slide 1
PhD Candidate: Zhijun (Julian) Liu
Research Progress Report
U R E P
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Colorado School of Mines
CSM
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Advisory Board Meeting, Nov 8 2019, Golden, Colorado
Investigation of Hindered Transport of Large Hydrocarbon Molecules in Nanoporous Materials

## Slide 2
1. Demonstrate and quantify the “hindered transport” of large hydrocarbon molecules through artificial membranes in the lab
2. Investigate factors that affect filtration process
  Temperature/Pressure/CO2
3. Investigate the mechanism of different effects on filtration
Research Objectives
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT

## Slide 3
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Experimental Setup
Hydrocarbons:
30% crude (Solute)
in toluene (Solvent)
ISCO Syringe Pump
Pressure Gauge
Gas Chromatography
(Mass Spectrometry)
Filtered
Hydrocarbon
Mixture
Gas Tank
Treated
Hydrocarbon
Mixture
Membrane:
Polyimide polymer
1.4nm pore size

## Slide 4
RE = 1 -
Ci,l
Retention Efficiency Calculation
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Ci,0
RE - Retention Efficiency of heavy component
Ci,l - Concentration of component i downstream
Ci,0 - Concentration of component i upstream at time 0,
i.e. in original sample

## Slide 5
What’s Happening on the Membrane Level
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Filtering of “large” molecules
Membrane
Membrane
Concentration Polarization
  Decrease flux
Upstream
Downstream
Flow direction
Notes: 𝑑𝑆𝑀<𝑑𝑝𝑜𝑟𝑒<𝑑𝐿𝑀

## Slide 6
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Raw Peak Area

## Slide 7
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Concentration Changes with Time

## Slide 8
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Concentration of Original vs. Downstream

## Slide 9
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Pressure Effect
Notes: Pressure effect agrees with literature

## Slide 10
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Temperature Effect

## Slide 11
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
CO2 Effect
Flowed pure toluene for 4 hours before tests to condition membranes

## Slide 12
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
CO2 Effect

## Slide 13
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Conclusions
(1) Temperature and pressure effect
  Increasing temperature and decreasing pressure led to lower retention efficiency
  Increasing temperature and increasing pressure led to higher flux
(2) CO2 effect
  CO2 reduced retention efficiency and increased flux
(3) The change of filtration due to P/T/CO2
  Change of temperature, pressure and addition of CO2 changes the diffusion and sieving of “solutes”

## Slide 14
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Advisory Board Meeting, Nov 8 2019, Golden, Colorado
Conduct filtration test using “stirred cell” so that upstream concentration on the membrane surface remains relatively constant
Future Work
Gas Pressurize
Hydrocarbon Mixture
Stir bar

## Slide 15
U R E P
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Colorado School of Mines
UNCONVENTIONAL RESERVOIR ENGINEERING PROJECT
Advisory Board Meeting, Nov 8 2019, Golden, Colorado